## Slide 1
Gary Stevens
Compact DUAL CHANNEL optical fibre amplifier for space communication applications
G&H Systems and Technology Group
& University of Glasgow

## Slide 2
Who we are
The Application
The Technology
Putting it together
The results
Radiation Testing
Future work
Contents

## Slide 3
      Company founded in 1948 in Ilminster, Somerset
      9 manufacturing sites, 3 in UK, 6 in USA
      Expertise in Acousto-optics, Electro-optics, Fibre-optics, Precision Optics and RF electronics
      STG based in Torquay - single team offering full system design services (optics, electronics, mechanical, modelling)
      Functional integration of G&H components into high-value products
      Design systems that can be transferred into serial production and ramped to high volumes
G&H Systems and Technology Group

## Slide 4
Missions Launched
Missions Planned
Product | Mission
Fibre Couplers and Fibre Modules | SMOS (ESA – Earth Observation)
Fibre Coupled DFB Laser | MISSE (NASA)
Fibre Coupled DFB (& Couplers) | LCRD (NASA)
Precision Optics | Mars Curiosity (NASA)
Precision Optics (superpolished) | Launch Vehicles (Classified)
Fibre Coupled AO | Classified
High Speed Photodetector | Classified
SM & MM Fibre Coupled Pumps | Classified
G&H Space Heritage

## Slide 5
STG Space Photonics current projects
  HIPPO High-Power Photonics for Satellite Laser Communications & On-Board Optical Processing
  MERLIN Multi‐gigabit, Energy‐efficient, Ruggedized Lightwave Engines for advanced on‐board digital processors
  BEACON Scalable & Low-Power Microwave Photonics for Flexible, Terabit Telecom Payloads & High-speed Coherent Inter-satellite Links
  MERMIG Modular CMOS Photonic Integrated Micro-Gyroscope
  TESLA-B / TESLA-C Terminal for Small Satellite LEO Application (ESA ARTES 5.2)
  RAD-EDFA Family of Optical Fiber Amplifiers for satellite communication systems and harsh environments (ARTES 5.2)
  ESA ECI 7524 Space validation of Rad‐Hard Erbium Optical Fibre Amplifiers
  ESA ECI 7586 Space Validation of DFB Laser Modules
European Projects
ESA
Projects

## Slide 6
Application
Next generation satellite communication system
  Laser communications replacing radio waves
  Extra security
  Increased data rates
  Lower electrical power, less weight, smaller
TESLA Optel-μ project

## Slide 7
Telcordia qualified sub-marine grade fused devices (taps, WDMs etc.)
  Space heritage (SMOS, Soil Moisture and Ocean Salinity mission)
Telcordia qualified high-rel isolators
Pump diodes now have space heritage
Biggest challenge is the Erbium Doped Fibre
Fibre Amplifier Technology

## Slide 8
Radiation Induced Attenuation (RIA) decreases transmission, pump absorption and gain
Standard telecoms fibres not suitable
Rad-hard Erbium Fibre
Radiation sensitivity dependent on:
  Doped fiber manufacturing method
  Doped fiber composition
  Doped fiber design / geometry
  Amplifier optical design
Intense R&D on rad-hard erbium-doped fibres

## Slide 9
OFA target specifications
Specification | Value
Input Power | -10 to 10 dBm
Input Wavelength | 1530 to 1565nm
Output power (EOL) | >20dBm
Switch time | 10Hz
Power consumption | <6.5W
Volume | 450cm3
Mass | 550g
Operational Temperature | -10 to 40oC
Radiation | 30kRad
Two EDFAs with separate outputs
Outputs can be combined via a switch and wavelength combiner into a single channel

## Slide 10
980nm pumping
Isolated input/output ports
Input and output power monitors
Switch used to combine the EDFAs onto a common output
Built-in redundancy
Up to 40dB gain
1) Optical design

## Slide 11
2) Electronics Design
Rad-hard custom design
Current driver and monitors
Telemetry
  Laser current monitor
  Laser power monitor
  Input power monitor
  Output power monitor
  Case temperature monitor
Tele-command
  Remote SET
  Remote ON/OFF
BOL Power consumption: 4.5W

## Slide 12
3) Module design & build
Optical network built ‘actively’
Electrical and optical connectors all on a single side
2mm thickness
Volume: 430cm3
Mass: 585g

## Slide 13
FEA Modelling
Shock and vibration modelling of housing
Modelling in a thermal vacuum
Heat management of pump diodes critical

## Slide 14
Amplifier Functional Performance
Chart: Pump Power / %
| 0.0 | 2.5 | 5.0 | 7.5 | 10.0 | 12.5 | 15.0 | 17.5 | 20.0 | 22.5 | 25.0 | 27.5 | 30.0 | 32.5 | 35.0 | 37.5 | 40.0 | 42.5 | 45.0 | 47.5 | 50.0 | 52.5 | 55.0 | 57.5 | 60.0 | 62.5 | 65.0 | 67.5 | 70.0 | 72.5 | 75.0 | 77.5 | 80.0 | 82.5 | 85.0 | 87.5 | 90.0 | 92.5 | 95.0 | 97.5 | 100.0
20mW | 5.3773 | 5.3769 | 5.5705 | 14.6477 | 25.5646 | 36.6724 | 47.8726 | 59.0759 | 70.2548 | 81.2641 | 91.876 | 103.2539 | 113.9146 | 124.0903 | 134.6091 | 145.2498 | 156.6973 | 166.3694 | 178.2216 | 187.9089 | 198.1516 | 208.4518 | 219.0776 | 228.5251 | 237.948 | 247.7382 | 256.7036 | 266.1867 | 275.5262 | 285.1 | 295.5277 | 304.1901 | 313.097 | 321.6095 | 329.8418 | 338.3733 | 345.9231 | 353.2754 | 360.9521 | 368.6782 | 374.9881
10mW | 1.6153 | 1.6156 | 1.6346 | 9.6405 | 20.3306 | 31.2312 | 42.3166 | 53.2807 | 64.3657 | 75.2451 | 85.8229 | 96.3812 | 106.3555 | 116.2344 | 126.9506 | 137.0012 | 147.0475 | 157.538 | 167.8582 | 178.3034 | 188.929 | 198.6547 | 208.2996 | 219.1798 | 227.9857 | 237.2909 | 247.1249 | 255.4328 | 264.1508 | 273.4624 | 281.7246 | 289.6376 | 299.519 | 307.2978 | 317.0128 | 325.881 | 333.2518 | 341.1387 | 347.8084 | 354.1831 | 360.5606
5mW | 0.23155 | 0.23264 | 0.24209 | 7.1919 | 17.6246 | 28.349 | 39.1045 | 49.7597 | 60.5971 | 71.2783 | 81.5042 | 91.9066 | 101.9158 | 112.0881 | 122.2366 | 131.3838 | 141.4211 | 152.1463 | 160.7366 | 170.6714 | 180.7583 | 189.959 | 198.9385 | 207.2902 | 217.0458 | 225.9586 | 234.1414 | 243.9836 | 252.8801 | 262.1338 | 271.378 | 279.4565 | 286.8977 | 293.9134 | 302.0889 | 309.6676 | 316.2704 | 322.9176 | 329.8969 | 336.0856 | 341.7911
2mW | 0.0026836 | 0.0027083 | 0.0029403 | 5.4949 | 15.3902 | 25.6333 | 35.9087 | 46.2164 | 56.3461 | 66.1442 | 75.915 | 85.115 | 94.6611 | 103.8629 | 113.1762 | 121.5991 | 131.3725 | 139.5592 | 149.3266 | 157.8274 | 167.2108 | 176.4022 | 183.5997 | 194.3537 | 202.834 | 210.4736 | 218.5214 | 226.504 | 234.0738 | 241.1032 | 248.6517 | 255.3671 | 262.3441 | 269.8926 | 277.0828 | 283.7743 | 290.9624 | 297.4611 | 303.8411 | 310.1507 | 316.1262
1mW | 0.00048774 | 0.00049271 | 0.0005341 | 4.6721 | 14.1941 | 23.8668 | 33.7152 | 43.0759 | 52.663 | 61.7583 | 70.9421 | 79.5446 | 88.1416 | 96.6283 | 104.4136 | 113.3143 | 122.0806 | 130.1373 | 139.3649 | 146.8895 | 154.6774 | 163.1642 | 170.0358 | 178.1297 | 184.732 | 193.3179 | 200.1239 | 206.5334 | 213.7248 | 221.7247 | 227.5516 | 234.823 | 240.4461 | 248.1407 | 254.0619 | 260.4205 | 267.1401 | 272.0958 | 277.7222 | 282.9896 | 288.0046
0.5mW | 0.00017297 | 0.00017669 | 0.00019707 | 4.1154 | 13.0811 | 22.2048 | 31.3317 | 40.1573 | 48.7122 | 57.2356 | 65.3609 | 73.7786 | 80.9535 | 88.6069 | 96.7537 | 104.0407 | 111.4642 | 118.145 | 125.1853 | 131.6974 | 139.4848 | 146.1191 | 153.2833 | 161.0605 | 167.2604 | 173.7611 | 179.4226 | 186.1919 | 192.2159 | 198.7521 | 204.4507 | 211.2341 | 215.8904 | 222.3315 | 227.7683 | 233.052 | 238.9886 | 243.694 | 248.3516 | 252.7223 | 256.8791
0.2mW | 5.765e-05 | 6.04e-05 | 7.8882e-05 | 3.4462 | 11.4801 | 19.3939 | 27.1342 | 34.5786 | 41.6819 | 48.7678 | 56.005 | 62.6037 | 69.1102 | 75.1224 | 81.6199 | 87.3824 | 93.8635 | 99.8633 | 106.267 | 112.2362 | 117.1468 | 123.8426 | 129.7402 | 135.3533 | 140.6957 | 146.4797 | 151.8006 | 156.7107 | 162.356 | 167.7501 | 172.4016 | 177.21 | 182.8685 | 186.6632 | 191.5625 | 195.8975 | 200.0753 | 204.2401 | 208.804 | 212.6851 | 216.6465
0.1mW | 2.7097e-05 | 2.9283e-05 | 4.4467e-05 | 2.9168 | 9.9748 | 16.7837 | 23.455 | 29.9135 | 35.8258 | 42.2935 | 48.1466 | 54.027 | 58.8155 | 64.6423 | 70.1125 | 75.891 | 80.5288 | 86.0151 | 91.2635 | 96.0809 | 101.6954 | 106.7456 | 111.996 | 116.8467 | 121.6722 | 126.2867 | 130.2894 | 135.012 | 140.5265 | 144.3574 | 148.1958 | 152.3225 | 156.3869 | 160.7363 | 165.0207 | 168.7441 | 172.5629 | 176.1985 | 180.3004 | 183.8092 | 187.3037
Input power
Chart: Pump Power / %
| 0.0 | 2.5 | 5.0 | 7.5 | 10.0 | 12.5 | 15.0 | 17.5 | 20.0 | 22.5 | 25.0 | 27.5 | 30.0 | 32.5 | 35.0 | 37.5 | 40.0 | 42.5 | 45.0 | 47.5 | 50.0 | 52.5 | 55.0 | 57.5 | 60.0 | 62.5 | 65.0 | 67.5 | 70.0 | 72.5 | 75.0 | 77.5 | 80.0 | 82.5 | 85.0 | 87.5 | 90.0 | 92.5 | 95.0 | 97.5 | 100.0
20mW | 4.0992 | 4.0985 | 4.2815 | 8.7451 | 14.0347 | 19.4009 | 24.8308 | 30.3148 | 35.5923 | 41.0291 | 46.203 | 51.5329 | 56.7676 | 61.6663 | 66.6521 | 71.7538 | 77.2833 | 81.9274 | 87.4626 | 91.9449 | 97.3586 | 102.4338 | 107.2006 | 111.9731 | 116.819 | 121.4642 | 126.2516 | 131.2707 | 135.8712 | 140.529 | 144.9127 | 149.6771 | 153.688 | 158.3355 | 162.2478 | 166.7233 | 170.8661 | 174.7864 | 179.1471 | 183.0032 | 187.0761
10mW | 1.3626 | 1.3618 | 1.3745 | 5.4499 | 10.601 | 15.877 | 21.2456 | 26.6462 | 31.9916 | 37.3621 | 42.3159 | 47.5002 | 52.4035 | 57.3274 | 62.5976 | 67.5192 | 72.2275 | 76.984 | 82.4492 | 86.9304 | 91.922 | 97.0477 | 101.4176 | 106.4448 | 111.2287 | 115.6789 | 120.4079 | 124.7078 | 129.5078 | 133.3364 | 138.3096 | 142.0636 | 147.015 | 151.2588 | 155.8638 | 159.986 | 164.1208 | 168.0767 | 171.7114 | 175.3071 | 178.8776
5mW | 0.21104 | 0.21197 | 0.22028 | 3.8679 | 8.8911 | 14.0793 | 19.2725 | 24.4088 | 29.6145 | 34.8333 | 39.8202 | 44.9436 | 49.8778 | 54.6561 | 59.8736 | 63.9728 | 69.4851 | 74.4113 | 78.6746 | 83.3014 | 88.3423 | 92.484 | 97.5375 | 101.8592 | 106.2968 | 111.3366 | 114.9564 | 119.6486 | 124.1561 | 128.6878 | 133.224 | 137.5125 | 141.5027 | 145.5114 | 149.5819 | 153.9106 | 157.2654 | 161.1226 | 165.1989 | 168.6616 | 172.2791
2mW | 0.0014518 | 0.0014657 | 0.00161 | 2.8351 | 7.6205 | 12.6519 | 17.6588 | 22.74 | 27.7653 | 32.5629 | 37.738 | 42.34 | 47.0861 | 51.5559 | 56.2572 | 60.8061 | 65.0705 | 69.7822 | 74.0626 | 78.7744 | 83.6638 | 87.6392 | 91.9747 | 97.0007 | 100.562 | 104.9996 | 109.0254 | 113.338 | 117.5118 | 121.6902 | 125.5107 | 129.3301 | 132.9671 | 137.0376 | 141.0038 | 144.8553 | 148.7194 | 151.8541 | 155.2881 | 158.6957 | 162.2822
1mW | 0.00018565 | 0.00018752 | 0.00020408 | 2.391 | 7.0062 | 11.7342 | 16.7207 | 21.4545 | 26.273 | 31.0419 | 35.4951 | 40.2296 | 44.6466 | 48.9603 | 53.1616 | 57.8033 | 62.4646 | 66.0683 | 70.6149 | 75.0915 | 79.6644 | 84.3222 | 88.0418 | 91.5607 | 96.082 | 100.0459 | 103.6519 | 107.5814 | 111.4398 | 115.4037 | 119.1256 | 122.891 | 126.1771 | 129.8577 | 133.5979 | 136.9745 | 140.7331 | 143.7668 | 147.0242 | 150.1956 | 153.4426
0.5mW | 6.7828e-05 | 7.0637e-05 | 7.9203e-05 | 2.0964 | 6.5194 | 11.1151 | 15.7334 | 20.3152 | 24.8955 | 29.508 | 33.925 | 38.1906 | 42.2035 | 46.4989 | 50.5167 | 54.6377 | 58.9102 | 62.569 | 67.0043 | 70.7204 | 74.7348 | 78.9051 | 82.8713 | 86.9075 | 90.5284 | 94.1941 | 97.6556 | 101.0839 | 104.4479 | 108.3831 | 111.4547 | 115.1651 | 118.0084 | 121.7315 | 125.1333 | 128.128 | 131.7696 | 134.637 | 137.5756 | 140.4223 | 143.2461
0.2mW | 2.3881e-05 | 2.5109e-05 | 3.5563e-05 | 1.8078 | 5.9788 | 10.2346 | 14.554 | 18.7058 | 22.8852 | 26.7221 | 30.908 | 34.878 | 38.5263 | 42.2242 | 46.0229 | 49.4994 | 53.2235 | 56.9993 | 60.517 | 64.1942 | 67.2268 | 71.2216 | 74.5902 | 77.9073 | 80.7747 | 84.1697 | 87.0176 | 90.2107 | 94.123 | 96.8401 | 99.7546 | 102.568 | 106.0995 | 108.4932 | 111.4145 | 114.1145 | 116.9303 | 119.4501 | 122.407 | 124.9361 | 127.5075
0.1mW | 1.1186e-05 | 1.3691e-05 | 2.2736e-05 | 1.6 | 5.464 | 9.3463 | 13.2501 | 17.0708 | 20.6719 | 24.5975 | 28.1927 | 31.6485 | 34.5837 | 38.0292 | 41.606 | 45.0595 | 47.9338 | 50.9881 | 54.0275 | 57.2689 | 60.4494 | 63.4556 | 66.76 | 69.5677 | 72.8102 | 75.1167 | 77.6194 | 80.481 | 84.0355 | 86.1814 | 88.7288 | 91.2475 | 93.7399 | 96.4903 | 99.3497 | 101.3351 | 103.9249 | 105.9275 | 108.5414 | 110.8422 | 113.1407
Input power
Chart: Pump Power / %
| 0.0 | 2.5 | 5.0 | 7.5 | 10.0 | 12.5 | 15.0 | 17.5 | 20.0 | 22.5 | 25.0 | 27.5 | 30.0 | 32.5 | 35.0 | 37.5 | 40.0 | 42.5 | 45.0 | 47.5 | 50.0 | 52.5 | 55.0 | 57.5 | 60.0 | 62.5 | 65.0 | 67.5 | 70.0 | 72.5 | 75.0 | 77.5 | 80.0 | 82.5 | 85.0 | 87.5 | 90.0 | 92.5 | 95.0 | 97.5 | 100.0
20mW | 1.5213 | 1.5224 | 1.5345 | 6.9867 | 13.636 | 20.4325 | 27.3072 | 34.1651 | 41.063 | 47.923 | 54.712 | 61.193 | 68.12 | 74.167 | 80.577 | 86.845 | 92.93 | 99.669 | 105.78 | 111.945 | 118.681 | 123.725 | 129.987 | 135.977 | 142.813 | 148.81 | 154.048 | 158.842 | 164.107 | 169.061 | 174.772 | 179.817 | 183.978 | 190.179 | 195.203 | 200.514 | 206.688 | 210.991 | 215.032 | 219.14 | 221.86
10mW | 0.30359 | 0.30458 | 0.31204 | 5.0262 | 11.5666 | 18.1878 | 24.9603 | 31.6653 | 38.121 | 45.022 | 51.409 | 57.632 | 64.094 | 70.282 | 77.554 | 82.684 | 88.602 | 95.23 | 100.953 | 106.607 | 113.839 | 119.402 | 125.683 | 131.263 | 136.538 | 142.772 | 149.015 | 154.505 | 159.356 | 164.035 | 168.627 | 173.367 | 178.479 | 182.904 | 186.939 | 191.403 | 196.135 | 200.643 | 205.783 | 209.531 | 213.071
5mW | 0.025212 | 0.025401 | 0.026789 | 3.9704 | 10.3252 | 16.7874 | 23.3024 | 29.7502 | 36.195 | 42.102 | 48.835 | 54.541 | 60.983 | 67.287 | 73.131 | 79.496 | 85.929 | 91.647 | 97.662 | 104.164 | 108.541 | 115.764 | 120.275 | 124.416 | 130.287 | 135.396 | 139.378 | 145.335 | 150.372 | 155.294 | 159.926 | 165.421 | 170.116 | 174.23 | 178.628 | 182.857 | 186.703 | 190.413 | 193.759 | 196.951 | 199.61
2mW | 0.0016182 | 0.0016329 | 0.0017484 | 3.2089 | 9.2573 | 15.4898 | 21.6752 | 27.6909 | 33.8025 | 39.751 | 45.142 | 51.101 | 56.894 | 61.95 | 66.944 | 73.082 | 78.287 | 82.637 | 88.127 | 94.09 | 99.405 | 103.314 | 109.204 | 114.892 | 118.157 | 124.494 | 129.346 | 132.873 | 136.609 | 142.62 | 144.584 | 148.969 | 153.212 | 156.639 | 161.048 | 164.439 | 168.6 | 172.474 | 175.575 | 178.328 | 181.601
1mW | 0.00042341 | 0.00042882 | 0.00046711 | 2.751 | 8.5605 | 14.4429 | 20.1235 | 26.0048 | 31.4391 | 36.722 | 41.992 | 47.646 | 52.151 | 56.468 | 62.296 | 67.136 | 70.936 | 76.621 | 80.37 | 85.597 | 89.071 | 93.302 | 97.9 | 101.99 | 106.995 | 109.787 | 113.733 | 117.568 | 121.925 | 125.776 | 129.086 | 133.132 | 137.128 | 140.682 | 144.023 | 146.676 | 149.198 | 151.849 | 154.266 | 156.387 | 157.663
0.5mW | 0.00015676 | 0.00015933 | 0.00018107 | 2.4249 | 7.7996 | 13.1687 | 18.3365 | 23.2707 | 28.2365 | 33.4497 | 37.646 | 41.315 | 46.182 | 49.361 | 53.976 | 57.739 | 62.448 | 66.048 | 69.862 | 72.776 | 77.803 | 81.926 | 86.031 | 87.407 | 92.131 | 96.285 | 99.581 | 103.75 | 106.261 | 109.8 | 112.254 | 114.785 | 118.042 | 120.636 | 122.986 | 125.804 | 128.497 | 130.863 | 133.308 | 135.955 | 138.266
0.2mW | 5.1718e-05 | 5.3888e-05 | 7.0153e-05 | 1.9495 | 6.5931 | 10.9956 | 15.1393 | 19.1062 | 23.2009 | 26.9029 | 30.4897 | 34.0214 | 37.38 | 40.954 | 44.136 | 47.176 | 50.305 | 54.363 | 57.052 | 60.727 | 63.943 | 68.253 | 70.706 | 73.733 | 77.178 | 78.92 | 83.206 | 84.669 | 87.301 | 90.882 | 92.693 | 95.168 | 97.715 | 100.522 | 103.09 | 105.75 | 108.411 | 110.671 | 112.934 | 114.847 | 116.444
0.1mW | 2.603e-05 | 2.7492e-05 | 4.1726e-05 | 1.637 | 5.6008 | 9.3442 | 13.0093 | 16.3296 | 19.815 | 22.9554 | 26.2835 | 29.3438 | 32.2064 | 35.508 | 39.125 | 42.223 | 44.857 | 47.203 | 51.157 | 53.301 | 56.324 | 59.051 | 62.084 | 64.298 | 67.396 | 69.586 | 72.728 | 76.137 | 77.676 | 80.769 | 82.561 | 85.382 | 88.796 | 90.996 | 93.498 | 95.633 | 97.752 | 99.485 | 101.221 | 102.851 | 104.282
Input power
1545nm results
1565nm results
Both channels combined

## Slide 15
Amplifier Temperature & Stability
Temperature testing -10o to 40oC.

## Slide 16
Radiation test setup
Similar amplifier sample built for radiation testing
Testing carried out at ALTER

## Slide 17
Pre-irradiation
GAIN
>20 dB over C-band
NF
Max 11 dB (1530 nm)
<6 dB (1550 nm)
<5 dB (1565 nm)

## Slide 18
Radiation (LEO scenario): 0 – 10 kRad (0 dBm input)
GAIN
Max gain drop 0.6 dB
>20 dBm over C-band
NF
<0.5 dB increase

## Slide 19
Radiation (LEO scenario): 0 – 10 kRad (0 dBm input)

## Slide 20
Radiation (GEO scenario): 0 – 100 kRad (0 dBm input)
GAIN
Max gain drop 3.44 dB
>18 dBm @ 60 krad
> 17 dBm @ 100 krad
NF
<2.17 dB increase

## Slide 21
Conclusions
EDFA design validated for LEO / GEO
  >20 dBm over C-band up to 10 krad (even in worst “passive” case)
  Gain drops:
    <0.6 dB up to 10 krad
    <3.44 dB up to 100 krad
Compact Dual Channel EDFA Built
  Provides up to 40dB gain
  Low mass, volume and power consumption
  Next Step: Proceed to EQM level development
    Component & Module level tests